Annex 4 to the TD

| TECHNICAL PARAMETERS OF THE SAMPLE PATTERN COINS (1ST TO 5TH TYPES) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Type of proof coin | 1st type CZK 200 normal quality | 2nd type CZK 200 proof quality | 3rd type CZK 1,000 normal quality patinated | 4th type CZK 10,000 normal quality patinated | 5th type CZK 1,000 proof quality |
| Shape | 1, round | 1, round | 1, round | 1, round | 1, round |
| Diameter and tolerance | 31.00±0.2 mm | 31.00±0.2 mm | 50.00±1 mm | 100.00±2 mm | 50.00±1 mm |
| Thickness and tolerance | not specified±0.3 mm | not specified±0.3 mm | not specified±3 mm | not specified±3 mm | not specified±3 mm |
| Weight and tolerance | 13.00 g-0+0.52 g | 13.00 g-0+0.52 g | 100.00 g-0+2 g | 1,000.00 g-0+20 g | 100.00 g-0+2 g |
| Coinage metal | AgCu 925:75 | AgCu 925:75 | Ag 999 | Ag 999 | Ag 999 |
| Tolerance | not specified-0+1% | not specified-0+1% | not specified-0+0.1% | not specified-0+0.1% | not specified-0+0.1% |
| Edge | plain | plain | plain | plain | plain |